# DRAGON ABRASIVES GROUP LTD

## Rm.2519,Core Mall Times Square, Nankai District Tianjin, China. Tel: 22-87899539 Fax:22-87899537

BROWN FUSED ALUMINA TECHNICAL DESCRIPTION

| TYPE | BFA-S |  | Resin Bonded Abrasives |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | BFA-V |  | Vitrified Bonded Grinding Wheel |  |  |  |
|  | BFA-B |  | Sandblasting |  |  |  |
|  | BFA-P |  | For Coated abrasives application |  |  |  |
| # Chemical Composition |  |  |  |  |  |  |
|  | Guarantee Content (%) |  |  |  | Typical Content (%) |  |
| Al2O3 | 95.00% min. |  |  |  | 96.07% |  |
| Fe2O3 | 0.20% max. |  |  |  | 0.17% |  |
| SiO2 | 1.20% max. |  |  |  | 0.83% |  |
| TiO2 | 1.80 – 3.00 % |  |  |  | 2.38% |  |
| CaO | 0.60% max. |  |  |  | 0.21% |  |
| MgO | 0.50% max. |  |  |  | 0.26% |  |
| ZrO2 |  |  |  |  | 0.08% |  |
| # Physical Properties |  |  |  |  |  |  |
| Color | Brown |  |  |  |  |  |
| Specific Gravity | 3.95 g/cm3 |  |  |  |  |  |
| Hardness | 9 Mohs |  |  |  |  |  |
| Bulk Density | BFA-S | BFA-V |  |  | BFA-B | BFA-P |
| F10 | 1.80-2.00 | 1.84-2.07 |  |  | 2.05-2.15 | 1.80-2.00 |
| F12 | 1.79-1.98 | 1.83-2.06 |  |  | 2.02-2.10 | 1.79-1.98 |
| F14 | 1.78-1.97 | 1.81-20.4 |  |  | 2.00-2.07 | 1.78-1.97 |
| F16 | 1.76-1.95 | 1.80-2.03 |  |  | 1.97-2.04 | 1.76-1.95 |
| F20 | 1.75-1.93 | 1.78-1.96 |  |  | 1.96-2.02 | 1.75-1.93 |
| F24 | 1.73-1.90 | 1.76-1.94 |  |  | 1.90-2.00 | 1.73-1.90 |
| F30 | 1.72-1.88 | 1.74-1.93 |  |  | 1.88-1.98 | 1.72-1.88 |
| F36 | 1.70-1.86 | 1.72-1.92 |  |  | 1.86-1.96 | 1.70-1.86 |
| F40 | 1.68-1.85 | 1.70-1.90 |  |  | 1.83-1.93 | 1.68-1.85 |
| F46 | 1.66-1.84 | 1.68-1.88 |  |  | 1.80-1.90 | 1.66-1.84 |
| F54 | 1.65-1.85 | 1.66-1.86 |  |  | 1.77-1.88 | 1.65-1.85 |
| F60 | 1.63-1.83 | 1.64-1.85 |  |  | 1.74-1.84 | 1.63-1.83 |
| F70 | 1.61-1.81 | 1.62-1.83 |  |  | 1.70-1.82 | 1.61-1.81 |
| F80 | 1.59-1.80 | 1.60-1.81 |  |  | 1.68-1.80 | 1.59-1.80 |
| F90 | 1.58-1.75 | 1.58-1.75 |  |  | 1.65-1.78 | 1.58-1.75 |
| F100 | 1.57-1.73 | 1.57-1.73 |  |  | 1.65-1.78 | 1.57-1.73 |
| F120 | 1.55-1.71 | 1.55-1.71 |  |  | 1.64-1.77 | 1.55-1.71 |
| F150 | 1.54-1.68 | 1.54-1.68 |  |  | 1.62-1.74 | 1.54-1.68 |
| F180 | 1.52-1.66 | 1.52-1.66 |  |  | 1.62-1.72 | 1.52-1.66 |
| F220 | 1.50-1.65 | 1.50-1.65 |  |  | 1.60-1.70 | 1.50-1.65 |